Semi-hot experimental facilities and methods employed in mechanical testing of irradiated reactor pressure vessels materials

Radim Kopriva, Miroslava Prochazkova

Nuclear Research Institute Rez plc.

Division of Integrity and Technical Engineering

Department of Mechanical Testing

250 68 Husinec – Rez

Czech Republic

e-mail : kor@ujv.cz, prm@ujv.cz

PACS : 	62.20.Mk	Fatigue, brittleness, fracture, and cracks

62.20.-x	Mechanical properties of solids

01.50.Pa	Laboratory experiments and apparatus

Keywords : 	fracture toughness, surveillance program, reconstutition, semi-hot laboratories

Abstract :

The main objective of this presentation is to characterise the design and construction of semi-hot cells laboratory for mechanical testing in the Nuclear Research Institute Rez. As described in this paper, the laboratory has all the necessary equipment and methods for postirradiation tensile, impact, fracture toughness and fractography measurements.

Within the Perfect subproject “Mechanics modeling”, results of mechanical properties as well as static fracture toughness results determined on the selected RPV materials in initial and irradiated conditions are summarized. Presented static fracture toughness test were carried out using shallow and deep fatigue precracked TPB specimens with dimensions 10x20 mm. For the testing, the ASTM E192105 method for reference temperature To determination was applied.