## Slide 1: Electronic structure and out-of-equilibrium electron dynamics of the quasi-two dimensional correlated metal BaNiS2
Niloufar Nilforoushan
Laboratoire de Physique des Solides, Université Paris-Sud, Orsay, France

## Slide 2
BaNiS2 a correlated metal
Electronic band structure
Temperature-dependence of the electronic structure
Out-of-equilibrium electron dynamics
Conclusion and Perspective
Nov 8th, 2017 ATTOLAB users meeting
Outline

## Slide 3: BaCo1-xNixS2
We are interested in:
Metallic precursor of Mott transition
multi-3d-orbital compound
Several Dirac-like bands
large Rashba splitting of the bands
Specific example of Mott material:
Nov 8th, 2017 ATTOLAB users meeting

## Slide 4
M M
band
QP
Hubbard band
The coherent part of the spectrum transfers to the incoherent part as T increases.
ARPES – BaNiS2, correlated metal (temperature dependent spectra measured with = 74eV at SPM beamline - synchrotron Elettra)
Nov 8th, 2017 ATTOLAB users meeting

## Slide 5
max
min
X
Nov 8th, 2017 ATTOLAB users meeting
ARPES – BaNiS2 Band structure ( = 70eV @ APE beamline - synchrotron Elettra)

## Slide 6
kz=0.0
kz=0.2
kz=0.6
kz=0.8
max
min
X
Fermi Surfaces
Nov 8th, 2017 ATTOLAB users meeting
ARPES – BaNiS2 Band structure (different photon energies @ APE beamline - synchrotron Elettra)

## Slide 7
Hidden spin polarization in centrosymmetric crystals with specific atomic site asymmetries.
Doubly degenerate bands: the two components could have opposite polarizations, each spatially localized on one of the two separate sectors forming the inversion partners.
X. Zhang et al., Nature Physics 10, 387–393 (2014)
Rashba spin-orbit coupling in asymmetric potentials:
M(A)
X(R)
M(A)
Rashba coupling of 0.25 eVÅ
band splitting up to 0.15 eV
D. Santos-Cottin et al., Nat. Commun. 7, 11258 (2016)
Nov 8th, 2017 ATTOLAB users meeting

## Slide 8: Theory vs. experiment
Nov 8th, 2017 ATTOLAB users meeting
D. Santos-Cottin et al., Nat. Commun. 7, 11258 (2016)
How does the electronic structure react with respect to the temperature or a photo-excitation?

## Slide 9
Probe pulse = 6.2eV on the FemtoARPES setup
J. Faure et al., Rev. Sci. Instrum. 83, 043109 (2012)
P polarization in order to observe the out-of-plane band:
S polarization to observe the
in-plane band:
Nov 8th, 2017 ATTOLAB users meeting

## Slide 10
Nov 8th, 2017 ATTOLAB users meeting
T=260K
T=110K
T=40K
T=110K
T=260K
T=40K
Out-of-plane band (spectrum with respect to temperature)
In-plane band (spectrum with respect to temperature)

## Slide 11
tr-ARPES study of the band
Electron dynamics (T=130k, h= 1.5eV, P=0.2 mJ/cm2 ; h= 6.2eV)
tr-ARPES sequences after photoexcitation with the pump pulse
Difference tr-ARPES images before and after photoexcitation: Electron(red) and hole(blue)
t= 50 fs
t= 150 fs
t= 500 fs
min
max
Negative delay
+1
-1
(a)
(b)
Nov 8th, 2017 ATTOLAB users meeting
t= 0 fs
t= 50 fs
t= 200 fs
t= 500 fs

## Slide 12
t= -175fs
(a)
+1
-1
t= -175fs
(b)
Nov 8th, 2017 ATTOLAB users meeting
The dynamics of the out-of-plane band
(c)
K-integrated spectrum

## Slide 13
t= -175fs
t= -175fs
Nov 8th, 2017 ATTOLAB users meeting
(c)
(a)
t= -175fs
+1
-1
(b)
The dynamics of the out-of-plane band
K-integrated spectrum

## Slide 14
t= -175fs
t= -175fs
Nov 8th, 2017 ATTOLAB users meeting
(c)
(a)
t= -175fs
+1
-1
(b)
(d)
The dynamics of the out-of-plane band
K-integrated spectrum

## Slide 15
t= 100 fs
t= 250 fs
t= 500 fs
tr-ARPES study of the band
Electron dynamics (T=130k, h= 1.5eV, P=0.2 mJ/cm2 ; h= 6.2eV)
tr-ARPES sequences after photoexcitation with the pump pulse
min
max
Difference tr-ARPES images before and after photoexcitation: Electron(red) and hole(blue)
Negative delay
+1
-1
Nov 8th, 2017 ATTOLAB users meeting
t= 0 fs
t= 100 fs
t= 300 fs
t= 700 fs

## Slide 16
(a)
(b)
(c)
Nov 8th, 2017 ATTOLAB users meeting
The dynamics of the in-plane band
K-integrated spectrum
(d)

## Slide 17
Temperature-dependent measurements vs. time resolved experiments
Solid-line curves: the k-integrated spectrum at 40 K subtracted from its counterpart at different temperatures.
Dashed-line curves: The k-integrated spectral weights for different time delays subtracted from the negative delay ones.
We observe that none of the curves belonging to the time evolution of the system correspond to a temperature difference spectrum.
b)
a)
Nov 8th, 2017 ATTOLAB users meeting

## Slide 18
125fs
max
min
Log(max)
Log(min)
+1
-1
(a)
(b)
(c)
(d)
and band (T=130k, h= 1.5eV, fluence 0.2 mJ/cm2)
18
Nov 8th, 2017 ATTOLAB users meeting
Difference tr-ARPES images
The dynamics of the excited electrons

## Slide 19: Conclusion
ARPES measurements:
Spectral weight transfer from the QP towards the Hubbard band with respect to the temperature
A full map of the Brillouin zone and the band dispersion
tr-ARPES measurements:
The relaxation time scale of the excited electrons above the Fermi level is about 600 fs for the d_(z^2 ) and d_(x^2−y^2 ) band along the GM direction.
Unoccupied states of the linearly dispersing bands along GM.
A comparison between the time-resolved data and the T-dependent evolution of the bands.
Nov 8th, 2017 ATTOLAB users meeting

## Slide 20: Conclusion
ARPES measurements:
Spectral weight transfer from the QP towards the Hubbard band with respect to the temperature
A full map of the Brillouin zone and the band dispersion
tr-ARPES measurements:
The relaxation time scale of the excited electrons above the Fermi level is about 600 fs for the and band along the GM direction.
Unoccupied states of the linearly dispersing bands along GM.
A comparison between the time-resolved data and the T-dependent evolution of the bands.
Nov 8th, 2017 ATTOLAB users meeting

## Slide 21: Perspective
A detailed time-resolved study of BaNiS2 with XUV probe pulses at Attolab: due to some geometric restrictions on the FemtoARPES setup, we cannot reach the Rashba split bands at 0.7-1 by 6.3 eV photon energy.
XUV probe energy and 1.5 eV pump pulse:
Reach the X point in the k-space.
Observe the dispersion of the predicted Rashba split bands above the Fermi level.
Pump with circularly polarized light: act on the spin degeneracy in these bands.
Nov 8th, 2017 ATTOLAB users meeting

## Slide 22: Acknowledgements
Marino Marsi (PhD advisor)
Evangelos Papalazarou, Marco Caputo, Lama Khalil, Zhesheng Chen
Alexei Victorovich Barinov, Ivana Vobornik, Jun Fujii, Pranab Das Kumar
David Santos-Cottin, Michele Casula, Yannick Klein, Andrea Gauzzi
Luca Perfetti, Christian Piovera
Nov 8th, 2017 ATTOLAB users meeting

## Slide 23
Thank you!
Iso-E surface of BaNiS2 at -0.2eV
Nov 8th, 2017 ATTOLAB users meeting